### GUIDE SPECIFICATION

## TC CLADDING( TERRACOTTA PANELS ON IBP FAST TRACK STONE( SUPPORT SYSTEM

# PART 1 - GENERAL

1.1. 	Scope

1.1.1.	Furnish all terracotta panels, wall panel support bracket pieces, cushions, attachment clips, shims, fasteners, vertical joint finish, and all other materials and labor necessary for complete wall cladding system installations as indicated on project drawings and specified herein.

1.1.2.	Related work specified elsewhere:

1.1.2.01.	Cast-In-Place and Plant-precast Concrete: Concrete supporting wall

1.1.2.02.	Unit Masonry Assemblies: Masonry supporting wall

1.1.2.03.	Thin Veneer Stone Assemblies: Thin cut veneer stone masonry

1.1.2.04.	Cold-Formed Metal and Structural Steel Framing: Steel frame supporting wall

1.1.2.05.	Framing and Sheathing: Wood frame supporting wall

1.1.2.06.	Sub-Frame: Panel System Support Stand-off framing

1.1.2.07. Building Insulation

1.1.2.08.	Weatherproofing

1.1.2.09.	Flashing

1.1.2.10.	Sealant

1.1.2.11. Exterior Curtain Walls, Windows, Glass, and Glazing

1.2. 	Guarantee

1.2.1.	Terracotta wall panel support system manufacturer shall guarantee for a period of five years from the date of purchase that the support system will be free of defects in materials and factory workmanship, and that defective materials will be repaired or replaced immediately, after proper notification.

1.2.2.	The installing contractor shall guarantee for a period of five years against faulty installation workmanship due to on-site errors

1.3. 	Submittals

1.3.1.	Submit assembly instructions and shop drawings for review and approval prior to system order showing pertinent details for installation; layout plan, terracotta panel sizes and coursing, alignments, attachments, supports, openings through system cladding, corner details, and adaptation of system to specific project.

1.4. 	Material Storage and Handling

1.4.1.	Store material in dry place, off the ground, where temperature will not exceed 90 degrees Fahrenheit.

1.4.2.	Handle material to prevent damage to finished surfaces. Do not install scratched or damaged components.

1.4.3.	After installation, protect finished surfaces from damage caused by ensuing work.

# PART 2 - PRODUCTS

2.1. 	Materials

2.1.1.	Acme TC Cladding Terracotta Panels: Lopo Plant manufactured terracotta clay panels as distributed by Acme Brick company: 3024 Acme Brick Plz, Fort Worth, TX 76109; Ph. 800-932-2263; Fax 817-332-1406; Email sweddle@brick.com

2.1.1.1. Sealed Joint Panel

2.1.1.1.a. Terracotta Panel Blends:

2.1.1.1.a.01. Desert Stone

2.1.1.1.a.02. Tumbleweed

# PART 2 – PRODUCTS CONTINUED

2.1.1.1.a.03. Sandstone

2.1.1.1.a.04. Amber Sky

2.1.1.1.a.05. Terra Cotta

2.1.1.1.a.06. Copperstone

2.1.1.1.a.07. Redwood

2.1.1.1.a.08. Russet

2.1.1.1.a.09. Coffee

2.1.1.1.a.10. Mahogany

2.1.1.1.a.11. Silver Mist

2.1.1.1.a.12. Pewter

2.1.1.1.a.13. Sierra Sands

2.1.1.1.a.14. Sable

2.1.1.1.a.15. Blue Manor

2.1.1.1.b. Terracotta Panel Finishes:

2.1.1.1.b.1. Flat

2.1.1.1.b.2. Scored

2.1.1.1.b.3. Linear

2.1.1.1.b.4. Sanded

2.1.1.1.b.5. Custom

2.1.1.1.c. Terracotta Panel Sizes:

2.1.1.1.c.1. 16 inches by 48 inches by 1-1/2 inches

2.1.1.1.c.2. Other

2.1.1.2. Rainscreen “Open” Joint Panel

2.1.1.2.a. Terracotta Panel Blends:

2.1.1.2.a.01. Desert Stone

2.1.1.2.a.02. Tumbleweed

2.1.1.2.a.03. Sandstone

2.1.1.2.a.04. Amber Sky

2.1.1.2.a.05. Terra Cotta

2.1.1.2.a.06. Copperstone

2.1.1.2.a.07. Redwood

2.1.1.2.a.08. Russet

2.1.1.2.a.09. Coffee

2.1.1.2.a.10. Mahogany

2.1.1.2.a.11. Silver Mist

2.1.1.2.a.12. Pewter

2.1.1.2.a.13. Sierra Sands

2.1.1.2.a.14. Sable

2.1.1.2.a.15. Blue Manor

2.1.1.2.b. Terracotta Panel Finishes:

2.1.1.2.b.1. Flat

2.1.1.2.b.2. Scored

2.1.1.2.b.3. Linear

2.1.1.2.b.4. Sanded

2.1.1.2.b.5. Custom

2.1.1.2.c. Terracotta Panel Sizes:

2.1.1.2.c.1. 400 millimeters by 1200 millimeters by 30 millimeters

2.1.1.2.c.2. Other

2.1.2.	IBP Fast Track Stone( System for Walls and Soffits: 6063-T6 extruded aluminum support bracket and clip system for masonry wall panels as manufactured by Innovative Building Products, Inc., an Acme Brick company,  3024 Acme Brick Plz, Fort Worth, TX 76109; Plant: 206 Dotson Street, Denton, TX, 76205.  Ph. 800-932-2263; Fax 817-332-1406; Email sweddle@brick.com

2.1.3.	Rubber cushion fittings: furnished with IBP Fast Track Stone(  System for Walls and Soffits.

2.1.4.	Plastic Shims: furnished with IBP Fast Track Stone(  System for Walls and Soffits.

# PART 2 – PRODUCTS CONTINUED

2.1.5.	Stainless Steel or Coated Screw Fasteners: furnished with IBP Fast Track Stone(  System for Walls and Soffits.

2.1.6.	Closed Cell Backer Rod: furnished with IBP Fast Track Stone(  System for Walls and Soffits.

2.1.7.	Sealant: Tremco Vulkem 116( Sealant, furnished with /IBP Fast Track Stone(  System for Walls and Soffits at sealed applications.

2.1.7.	Metal Vertical Joint Blocker Flashing: furnished with rainscreen “open” joint TC Cladding terracotta panels

# PART 3 - EXECUTION

3.1.	Field Conditions

3.1.1.	Verify all applicable field dimensions and adjust as necessary to accommodate wall and/or soffit system.

3.1.2.	Examine sub-frame and/or backing wall and/or ceiling structure on which support system will be installed. Confirm that sub-frame and backing wall and/or ceiling meet requirements and alignment tolerances of cast-in place concrete, plant-precast structural concrete, unit masonry assemblies, cold-formed metal framing, and/or framing and sheathing section/s of the specifications. Correct any conditions which are not constructed according to specification tolerance installation instructions and approved shop drawings furnished by support system manufacturer.

3.1.3.	Assure that face of backing wall is adequately prepared to act as drainage surface in accordance with the requirements of the weatherproofing section of the specifications.

3.2.	Installation

3.2.1	Install bracket supports onto sub-frame or directly to backing wall and/or ceiling with appropriate fasteners in accordance with applicable code and manufacturer’s recommendations, plumb and true to line, and shimmed where and as necessary to maintain no greater than 1/8” offset of adjoining panel faces.

3.2.2.	Apply cushion fittings to mounting edges of brackets and clips. Set bottom grooves of kerfed terracotta panels onto bracket cushions. Set cushioned clips over top lip edge of panels and tilt into place until panel clip prongs snap secure into bracket prongs. Repeat process for each panel, positioning them according to installation drawings furnished by manufacturer.

3.2.3.	Assure that openings through terracotta panels supported on system are properly flashed in accordance with installation drawings and the requirements of the flashing section of the specifications.

3.2.4.	Install backer rod at all joints for sealed joint applications. Perimeter edges of stone panels can be masked off with tape and then apply sealant to fill between terracotta panels. Masking edges with tape before applying sealant is OPTIONAL. Remove tape to clean up edges after sealant has cured. Perform all sealant work in accordance with the requirements of the sealant section of the specifications.

3.2.5.	Install metal vertical joint blocker flashing at ends of panels for rainscreen “open” joint applications.

3.3.	Clean-up

3.3.1.	Clean all dirt, marks, and sealant from terracotta panels using methods appropriate for terracotta clay material and per supplier’s recommendations.

3.3.2.	Touch-up chipped and scratched surfaces per supplier’s guidelines or remove and replace damaged panels as directed by the architect.

***END OF SECTION***