### GUIDE SPECIFICATION

## TC CLADDING( TC SUNSHADE TERRACOTTA BAGUETTES ON ALUMINUM SUPPORT TUBE

# PART 1 - GENERAL

1.1. 	Scope

1.1.1.	Furnish all terracotta baguettes, baguette support tube pieces, attachment brackets or clips, clip fasteners, baguette support framing and fasteners for attachment to building structure, and all other materials and labor necessary for complete baguette installations as indicated on project drawings and specified herein.

1.1.2.	Related work specified elsewhere:

1.1.2.01.	Cast-In-Place and Plant-precast Concrete: Concrete supporting wall

1.1.2.02.	Unit Masonry Assemblies: Masonry supporting wall

1.1.2.03.	Cold-Formed Metal and Structural Steel Framing: Steel frame supporting wall

1.1.2.04. Metal Fabrications

1.1.2.05.	Framing and Sheathing: Wood frame supporting wall

1.1.2.06.	Sub-Frame: Panel System Support Stand-off framing

1.1.2.07.	Weatherproofing

1.1.2.08.	Flashing

1.1.2.09.	Sealant

1.1.2.10. Exterior Curtain Walls, Windows, Glass, and Glazing

1.2. 	Guarantee

1.2.1.	Terracotta baguette and support hardware manufacturer shall guarantee for a period of five years from the date of purchase that the support fixtures and baguettes will be free of defects in materials and factory workmanship, and that defective materials will be repaired or replaced immediately, after proper notification.

1.2.2.	The installing contractor shall guarantee for a period of five years against faulty installation workmanship due to on-site errors.

1.3. 	Submittals

1.3.1.	Submit assembly instructions and shop drawings for review and approval prior to system order showing pertinent details for installation; layout plan and details, terracotta baguette profiles and sizes, alignments, attachments, supports, corner detail treatment, and adaptation of system to specific project.

1.4. 	Material Storage and Handling

1.4.1.	Store material in dry place, off the ground, where temperature will not exceed 90 degrees Fahrenheit.

1.4.2.	Handle material to prevent damage to finished surfaces. Do not install scratched or damaged components.

1.4.3.	Make necessary arrangements after installation to protect finished surfaces from damage caused by ensuing work.

# PART 2 - PRODUCTS

2.1. 	Materials

2.1.1.	Acme TC Cladding TC Sunshade Terracotta Baguettes: Lopo Plant manufactured terracotta clay baguettes as distributed by Acme Brick Company: 3024 Acme Brick Plaza, Fort Worth, TX 76109; Ph. 800-932-2263; Fax 817-332-1406; Email tccladding@brick.com

2.1.1.1. Baguette

2.1.1.1.a. Terracotta Baguette Blends:

2.1.1.1.a.01. Linen (color no. 001)

2.1.1.1.a.02. Desert Stone (color no. 002)

# PART 2 – PRODUCTS CONTINUED

2.1.1.1.a.03. Tumbleweed (color no. 003)

2.1.1.1.a.04. Patagonia (color no. 011)

2.1.1.1.a.05. Sandstone (color no. 230)

2.1.1.1.a.06. Honeycomb (color no. 232)

2.1.1.1.a.07. Amber Sky (color no. 235)

2.1.1.1.a.08. Spicewood (color no. 236)

2.1.1.1.a.09. Papaya (color no. 238)

2.1.1.1.a.10. Pumpkin Cider (color no. 630)

2.1.1.1.a.11. Colonial Maple (color no. 632)

2.1.1.1.a.12. Terra Cotta (color no. 633)

2.1.1.1.a.13. Copperstone (color no. 635)

2.1.1.1.a.14. Redwood (color no. 639)

2.1.1.1.a.15. Black Cherry (color no. 692)

2.1.1.1.a.16. Nutmeg (color no. 770)

2.1.1.1.a.17. Coffee (color no. 773)

2.1.1.1.a.18. Mahogany (color no. 777)

2.1.1.1.a.19. Chocolate (color no. 789)

2.1.1.1.a.20. Silver Mist (color no. 880)

2.1.1.1.a.21. Gauntlet Gray (color no. 883)

2.1.1.1.a.22. Pewter (color no. 884)

2.1.1.1.a.23. Sierra Sands (color no. 886)

2.1.1.1.a.24. Sable (color no. 889)

2.1.1.1.a.25. Dragon Glass (color no. 899)

2.1.1.1.a.26. Coastal Jetty (color no. 994)

2.1.1.1.a.27. Stirling (color no. 996)

2.1.1.1.a.28. Blue Manor (color no. 999)

2.1.1.1.b. Terracotta Baguette Profiles:

2.1.1.1.b.1. Square: 50 millimeters by 50 millimeters

2.1.1.1.b.2. Rectangle: 50 millimeters by 100 millimeters

2.1.1.1.b.3. Large Rectangle: 50 millimeters by 150 millimeters

2.1.1.1.b.4. Fin

2.1.1.1.b.5. Custom

2.1.1.1.c. Terracotta Baguette Finishes:

2.1.1.1.c.1. Flat

2.1.1.1.c.2. Sanded

2.1.1.1.c.3. Custom

2.1.1.1.d. Terracotta Baguette Sizes:

2.1.1.1.d.1. millimeters tall by millimeters wide by millimeters long

2.1.1.1.d.2. Other

2.1.2.	TC Sunshade Terracotta Baguette Support Hardware: 6063-T5 extruded aluminum support clip, square support tube, and attachment clip, stainless steel end bracket, EPDM cushion, and 6063-T5 aluminum end hook with stainless steel friction fit holding spring and aluminum receiver hardware for terracotta baguettes provided by Acme Brick Company: 3024 Acme Brick Plaza, Fort Worth, TX 76109; Ph. 800-932-2263; Fax 817-332-1406; Email tccladding@brick.com (Note: TC Cladding does not typically provide baguette support framing such as knife plates and out-rigger members nor installation labor)

2.1.2.1. 6063-T5 Aluminum Support Clip

2.1.2.2. 6063-T5 Aluminum Support Square Tube

2.1.2.3. 6063-T5 Aluminum Attachment Clip

2.1.2.4. Stainless Steel End Brackets

2.1.2.4.a. Single Tube Mount End Bracket

2.1.2.4.b. Single Tube Mount Corner End Bracket

2.1.2.4.c. Double Tube Mount end Bracket

2.1.2.4.d. Double Tube Mount Corner End Bracket

(Note: brackets can optionally be powder coated to project specified color by supplier prior to being delivered to installer)

2.1.2.5. EPDM Cushion

# PART 2 – PRODUCTS CONTINUED

2.1.2.6. 6063-T5 Aluminum Interior Application Bracket Fixtures

2.1.2.6.a. End Hook with stainless steel friction fit holding spring

2.1.2.6.b. Receiver Wall Mount

2.1.3.	Rubber or PTFE Washers: furnished with TC Sunshade mounting hardware.

2.1.4.	Stainless Steel or Coated Screw Fasteners and Washers: furnished with TC Sunshade mounting supports.

# PART 3 - EXECUTION

3.1.	Field Conditions

3.1.1.	Verify all applicable field dimensions and adjust as necessary to accommodate terracotta baguette and hardware installation.

3.1.2.	Examine knife plate or out-rigger sub-frame, curtain wall, and/or backing wall structure on which baguette supports will be installed. Confirm that sub-frame, curtain wall frame, and backing wall meet requirements and alignment tolerances of cast-in place concrete, plant-precast structural concrete, unit masonry assemblies, cold-formed metal framing, and/or wood framing and sheathing section/s of the specifications. Correct any conditions which are not constructed according to specification tolerance installation instructions and approved shop drawings furnished by support system manufacturer.

3.1.3.	Provide the Architect with a written notification of any deviations from manufacturer’s recommended installation tolerances and conditions when corrections are the responsibility of another installer and proceed with work only after unsatisfactory issues have been corrected.

3.2.	Installation (note: instructions for hardware different from what is being used on the project are to be removed)

3.2.1.	Install knife plate, out-rigger, or other support frame in accordance with fabricator’s or manufacturer’s instructions and approved shop drawings to specified installation tolerances.

      - Baguettes Mounted with Internal Clip Angles without Support Tubing

- Use an internal clip angle placed into each end of a baguette to mark the location for drilling attachment holes when baguettes do not have holes pre-drilled or when field cut pieces are employed. Drill attachment holes through the ends of the baguettes at the marked locations as required. Skip to step ‘B’ for baguettes with attachment holes already provided.

- Set an internal clip angle in place at the end of the baguette. Align the slot in the angle with the drilled hole through the wall of the baguette at one end. Thread a carriage bolt through the slot of the internal clip angle and the hole through the baguette. Install a PTFE or rubber washer over the bolt end first and then an attachment clip angle. Next place a metal washer over the bolt end followed by a lock washer and twist a nut over the bolt end to finger tighten the attachment pieces in place. Adjust the bolted pieces over the slot through the attachment clip as necessary to square the clip up with the baguette edges and align it to the sub-frame where the assembly will be mounted and then firmly tighten the bolt nut into place taking care not to over-tighten it.

- Repeat the installation of attachment pieces at the opposite end of the baguette.

- Connect the attachment clips to the sub-frame that the baguette is to be mounted onto by fastening with bolts through the slots of the attachment clips and slots in the mounting frame or with self-drilling screws into the metal of the sub-framing.

3.2.1.2.	Baguettes Mounted with Clip Angles Attached to Support Tubing

- Thread a length of aluminum square support tubing through the center of the baguette. The length of the tube should match the length of the baguette. Use a piece of tube of sufficient length to match the baguette if a piece is short or cut the tube as necessary if the piece is longer than baguette.

# PART 3 – EXECUTION CONTINUED

- Mark the location for drilling attachment holes as shown on shop drawings when baguettes do not have holes pre-drilled or when field cut pieces are employed. Drill attachment holes through the ends of the baguettes at the marked locations as required. Skip to step ‘C’ for baguettes with attachment holes already provided.

- Align the slot in an attachment clip angle with the drilled hole through the wall of the baguette at one end. Place a PTFE or rubber washer between the angle and the baguette with its hole aligned to the other holes. Set a metal washer over the threads of a self-drilling screw and drill the screw in place

through the baguette hole into the square support tube at the inside of the baguette. Adjust the screwed together pieces over hole through the baguette as necessary to square the clip up with the baguette edges and align it to the sub-frame where the assembly will be mounted and then firmly tighten the screw into place taking care not to over-tighten it.

- Repeat the installation of attachment pieces at the hole at the opposite end of the baguette.

- Connect the attachment clips to the sub-frame that the baguette is to be mounted onto by fastening with bolts through the slots of the attachment clips and slots in the mounting frame or with self-drilling screws into the metal of the sub-framing.

3.2.1.3.	Baguettes Mounted on Support Tubing Attached to End Brackets

- Thread aluminum square support tubing through center of the baguette. The length of tube should match the length of the baguette. Use piece of tube of sufficient length to match baguette if piece is short or cut tube as necessary if piece is longer than baguette.

- Fit a piece of EPDM cushion between support tubing and inside core opening of baguette at each end to wedge tubing in place.

- Place the channel shaped portion of an end bracket into the support tube end at each end of the baguette to prepare it to be secured to the building sub-frame where it is to be installed.

- Connect the end brackets placed at each end of the baguette with bolts or self-drilling screws through the two attachment slots at each bracket to the sub-framing where the baguette is to be installed.

3.2.1.4.	Baguettes Supported by Interior Wall Brackets: not intended for exterior or overhead applications

- Fit the spring blades of an end hook fixture into each end of the baguette. The fixtures should be pushed into the baguette until there is about a 1/8” to 3/16” space between the core opening of the baguette and the surface of the end hook closest to the opening. Adjust the position of the end hook to align the hook portion protruding out of the baguette core parallel to the end face of the baguette.

- Attach an end hook receiver wall mount with two screws to the sub-framing or wall surface where each end of the baguette is to be installed according to the shop drawing layout for the project.

- Slide the end hooks at the ends of the baguette into the receiver wall mount brackets to set the baguette in place.

3.2.2.	A single support rod is used for 50mm x 50mm profile baguettes. Some larger profiles require two support rods and associated larger brackets or clips for attachment. The project shop drawings will detail and provide installation instructions for specific hardware requirements for larger or custom profiles.

3.3.	Clean-up

3.3.1.	Clean all dirt and marks from terracotta baguettes using methods appropriate for terracotta clay material and per supplier’s recommendations.

3.3.2.	Touch-up chipped and scratched surfaces per supplier’s guidelines or remove and replace damaged baguettes as directed by the architect.

***END OF SECTION***